## Slide 1: Dry Etch Chemistry - Si, SiO, & SiN
September 17th, 2024
Yongchul Yoo
Ph.D. in materials Engineering
Notes: topic

## Slide 2: Etch Chemistry
Etchant
- Halogen based feed gas in dry etch
(F, Cl, Br, CxFy, HBr, BCl3, etc.)
Additive gas
- Reactive
(O2, H2, N2, CO, CH4, etc.)
Additive gas
- Nonreactive
(Ar, He, Xe, etc.)
Polymer formation - Anisotropic - Selectivity
Etchant concentration
- Selectivity
Ionization
Dilution of etchant
Heat transfer
Etch materials by chemical reactions
Provide the polymer precusor (C, H)

## Slide 3: Etch Chemistry for Anisotropic/Selectivity
Anisotropic?
Prevent isotropic etching
  Gas chemistry for passivation layer
    - e.g. Polymer precusor, C
SF6
NF3
CxFy
O2
SiF4/O2
Anisotropic than F
Cl2
Br2
Isotropic, Fast etching (F > Cl >Br)
Anisotropic
CH4
Si
SiO
H2
Si
CHF
Selectivity?
Adjust etchant by additive gas to favor/suppress etching of specific films
O2
  Increase in F (etchant) up to certain level
  Formation of oxide layer (if too much)
H2
  Decrease of F in CF plasma (HF)
  Polymer formation on Si
N2: Faciliatation of nitride etch (NO)
Anisotropic
O2
H2
N2
Faster Si etch
Faster SiO etch
Faster SiN etch
Etching Si, SiO, and SiN
Selectivity control for Si, SiO, SiN
Mitigation of microtrench
O2
Si,
Si: SiO selectivity
HBr
Si, SiO, and SiN
Etch control
Cryogenic condition
Notes: The purpose of this project is to improve corrosion by performing the supersonic laser deposition of CrNeNiTi high entropy alloy coating on stainless steel 316.
This presentation deals with
Nuclear energy future, and issue
Mitigation approach to improve the issue
What desired properties are
Coating method
Selected coating method
Candidate processing method per current coating
How to demonstrate the research
outcome

## Slide 4: Etchant & additive example
Film 1 | Film2 | Selectivity (Film1 to Film2) | Goal | Etchant | Additive | Mechanism/Effect | Reference
Si | - | - | Anisotropic | SF6 | O2 | In cryogenic condtion, passivating layer, SiOxFy, Sulfur(S): no significant contribution to passivation layer At room temperature: no passivation layer | Passivation mechanisms in cryogenic SF6/O2 etching process
Si | - | - | Anisotropic | NF3 | H2 | Passive layer: (NH4)2SiF6 Etching needs more than 40% of NF3 | Reactive ion etching of crystalline silicon using NF3 diluted with H2
SiO | PR | 1.3 | Selectivity | SF6 | CH4 | Passive layer: CHxFy layer | Study of SiO2 etching processing with CH4/SF6 plasmas
Si | SiO | 10 | Selectivity | CF4 | O2 | Up to about 23%, increase in F atom (CF3 + O2 reaction) Above 23% of oxygen, F decreases: electron energy reduction, oxidized Si surface | Downstream Etching of Si and SiO2 Employing CF4/O2 or NF3/O2 at high temperature
SiO | Si | 45 (at high H2) | Selectivity | CF4 | H2 | CF4+ H2 : Scavange Radical (F) (HF formation) Si etch: F, SiO2: Both F and C contribute to etch | Parameter and Reactor Dependence of Selective Oxide RIE in CF4+ H2
SiO | Si | 15 | Selectivity | CHF3 | CH4 | F scavange by H atoms for CH2 same as H2 (main etching source for Si SiO: ion etching (sputtering) is more effective Produce a carbon rich fluorocarbon film on Si | SiO2/Si SELECTIVITY IN HIGH DENSITY CHF3 /CH4 PLASMAS : ROLE OF THE FLUOROCARBON LAYER
SiN | SiO | 9 | Selectivity | CF4 | O2/N2 | SiN: NO reacts with N (solid) in SiN SiO2: independent of NO | Role of nitrogen in the downstream etching of silicon nitride
SiN | Si | 2 | Selectivity | CHF3 | O2 | SiN: O2 acts as 1) Reactive F atoms by producing CO, CO2, 2) Removal of N, 3) Flurocarbon film formation on the surface Si : Oxide layer formation to provide selectivity against SiN | Vertical sidewall of silicon nitride mask and smooth surface of etched-silicon simultaneously obtained using CHF3/O2 inductively coupled plasma
SiN | Si | 16 | Selectivity | CHF3 | N2 | Dilute the polymer-forming radicals Generates abundant N atoms to etch N from SiN | Selective reactive ion etching of silicon nitride over silicon using CHF3 with N2 addition
Anisotropy of Si & Selectivity studies between Si, SiN, and SiO

## Slide 5: Film Dependency Etching
Crystallographic dependency for etch rate
  The different area densities of silicon atoms (or Si –Si bonds) at the surface. The (111) orientation has a higher density than the (100) orientation, which reduces Cl or Cl penetration into the lattice for 111, leading to a lower etch rate
Doped film dependency etching : case study on (Si, Cl2 etchant)
Ec
Ev
Ei
EF
Ev
Ec : Conduction band, Ei : Intrinsic, Ev : valence band, EF : Fermi level (50% propability of electrons' occupation at any given time)
N doped : Fermi level, EF , approaches conduction band
Ec
EF , Ei
Undoped
Permits more available electron transfer from the silicon surface to chemisorbed Cl → Higher etch rate
P, Sb, As : n doping (electron)
Reference: PRINCIPLES OF PLASMA DISCHARGES AND MATERIALS PROCESSING, Doping and crystallographic effects in Clatom etching of silicon

## Slide 6: Film Dependency Etching
Ion dependency for etch rate
  Higher etch rate by Cl2+/Cl2 > Ar+/Cl2
Cl2+ bombardment → Highly disordered, roughened layer with small subsurface voids. Such a layer contains more binding sites for adsorption by neutral Cl and Cl2
Ar+ bombardment → Disordered but dense damaged layer
Reference: Plasma etching: Yesterday, today, and tomorrow

## Slide 7: H2 & O2 Effect on Etching of SiO2 & Si
Hydrogen Effect
Decrease in F by H+F → HF
Thicker film formation on Si than SiO2
Oxygen effect
  Up to certain level, increase in atom F by CxFy+ O → Liberate F
  Above the certain level, decrease in atom F caused by quenching effect by high flow of dilution gas, oxidation of Si
Controlling behavior of Si and SiO
  Si : Etching by F
  SiO : Etching by both F and C, more efficient for sputtering by higher ion energy
CF4/H2
CF4/O2
  Reference : Parameter and Reactor Dependence of Selective Oxide RIE in CF4+ H2
  Reference : Plasma etching of Si and Si02-The effect of oxygen additions to CF4 plasmas

## Slide 8: Fluorocarbon film behavior
Low bias voltage is effective to deposit polymers
The ratio of carbon and fluoride (x/y) C3F6 vs C2F6 → Thicker depostoin for C3F6
H inclusion further deposits CHF3, and C3F6/H2 → Thicker deposition
Passivation layer
Reactants during ion bombardment
Reference: Plasma etching: Yesterday, today, and tomorrow